## Slide 1: Technology Nodes & Scaling
EECS 277A

## Slide 2
B. Davari, R. Dennard and G. Shahidi, "Cmos Scaling for High Performance and Low Power-the Next Ten Years", Proceedings of the IEEE, 83, 595-606, (2002).

## Slide 3
Y. Taur, D. Buchanan, W. Chen, D. Frank, K. Ismail, S. Lo, G. Sai-Halasz, R. Viswanathan, H. Wann and S. Wind, "Cmos Scaling into the Nanometer Regime", Proceedings of the IEEE, 85, 486-504, (2002).

## Slide 7: RF/AMS
Table RFAMS1 RF and Analog Mixed-Signal CMOS Technology Requirements |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Year of Production | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024
Performance RF/Analog [1] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Supply voltage (V) [2] | 1.1 | 1.05 | 1.05 | 1.05 | 1 | 0.95 | 0.95 | 0.95 | 0.85 | 0.85 | 0.85 | 0.85 | 0.75 | 0.75 | 0.75 | 0.75
Tox (nm) [2] | 1.2 | 1.2 | 1.2 | 1.2 | 1.10 | 1.10 | 1.10 | 1.10 | 1.10 | 1.00 | 1.00 | 0.90 | 0.90 | 0.80 | 0.80 | 0.70
Gate Length (nm) [2] | 38 | 38 | 32 | 29 | 27 | 22 | 18 | 17 | 15 | 14 | 13 | 12 | 11 | 9.7 | 8.9 | 8.1
gm/gds at 5·Lmin-digital [3] | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30
1/f-noise (µV²·µm²/Hz) [4] | 100 | 90 | 80 | 70 | 70 | 60 | 50 | 50 | 40 | 40 | 40 | 30 | 30 | 30 | 20 | 20
s Vth matching (mV·µm) [5] | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 4 | 4 | 4 | 4 | 4
Ids (µA/µm) [6] | 9 | 9 | 8 | 7 | 7 | 6 | 5 | 4 | 4 | 3 | 3 | 3 | 2 | 2 | 2 | 2
Peak Ft (GHz) [7] | 240 | 240 | 280 | 310 | 340 | 400 | 480 | 520 | 570 | 630 | 680 | 750 | 820 | 890 | 970 | 1060
Peak Fmax (GHz) [8] | 290 | 290 | 340 | 380 | 420 | 510 | 610 | 670 | 740 | 820 | 900 | 990 | 1090 | 1200 | 1320 | 1450
NFmin (dB) [9] | 0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2
Precision Analog/RF Driver [1] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Supply voltage (V) | 2.5 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.5 | 1.5 | 1.5 | 1.5 | 1.5 | 1.5
Tox (nm) [10] | 5 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6
Gate Length (nm) [10] | 250 | 180 | 180 | 180 | 180 | 180 | 180 | 180 | 180 | 180 | 130 | 130 | 130 | 130 | 130 | 130
gm/gds at 10·Lmin-digital [11] | 220 | 160 | 160 | 160 | 160 | 160 | 160 | 160 | 160 | 160 | 110 | 110 | 110 | 110 | 110 | 110
1/f Noise (µV²·µm²/Hz) [4] | 1000 | 360 | 360 | 360 | 360 | 360 | 360 | 360 | 360 | 360 | 270 | 270 | 270 | 270 | 270 | 270
s Vth matching (mV·µm) [5] | 9 | 6 | 6 | 6 | 6 | 6 | 6 | 6 | 6 | 6 | 5 | 5 | 5 | 5 | 5 | 5
Peak Ft (GHz) [7] | 40 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 70 | 70 | 70 | 70 | 70 | 70
Peak Fmax (GHz) [8] | 70 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 90 | 120 | 120 | 120 | 120 | 120 | 120
Availability of optional analog / High-voltage FETs | limited | limited | common | common | wide | wide | wide | wide | wide | wide | wide | wide | wide | wide | wide | wide
 |  |  |  |  |  |  | switch to UTB FD or DG device |  |  |  |  |  |  |  |  | 
Manufacturable solutions exist, and are being optimized |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Manufacturable solutions are known |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Interim solutions are known | ¿ |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Manufacturable solutions are NOT known |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |